|  |  |  |  |
| --- | --- | --- | --- |
| **Process** | **Loop** | **Traveler** | **Sequence** |
| Optical Inspection |  | C75-CAV-INSP-OPTK |  |
| RF Inspection | C75-CAV-TUNE |  |
| CMM Cavity Inspection | C75-CAV-INSP |  |
| Thickness Measurements |  | C75-CAV-CHEM-THK |  |
| CBP (60u medium) |  | C75-CHEM-CAV-CBP |  |
| USC |  | C75-CHEM-CAV-DEGR |  |
| CBP (fine – surface finishing) |  | C75-CHEM-CAV-CBP |  |
| USC |  | C75-CHEM-CAV-DEGR |  |
| Thickness Measurements |  | C75-CAV-CHEM-THK |  |
| HEP – 40u warm A |  | C75-CAV-CHEM-HEP |  |
| USC |  | C75-CHEM-CAV-DEGR |  |
| Heat (450C/3h + 800C/3h) |  | C75-CAV-HEAT |  |
| HEP – 30u warm A  Or 15u warm A + 15u cold A |  | C75-CAV-CHEM-HEP |  |
| USC |  | C75-CHEM-CAV-DEGR |  |
| Thickness Measurements |  | C75-CAV-CHEM-THK |  |
| RF Inspection |  | C75-CAV-TUNE |  |
| CMM Inspection (Flange Flatness & surface finish) | C75-CAV-INSP |  |
| Flange Lapping |  | C75-CAV-CHEM-FLAP |  |
| Flange BCP & HF | C75-CAV-CHEM-BCP-FLNG |  |
| Cavity USC | C75-CHEM-CAV-DEGR |  |
| Flange Inspection | C75-CAV-INSP? |  |
| USC (Liquinox and DI) |  | C75-CHEM-CAV-DEGR |  |
| HPR – 4 pass |  | C75-CAV-CHEM-HPR |  |
| Assembly |  |  |  |
|  |  |  |  |
|  |  |  |  |
|  |  |  |  |
|  |  |  |  |