## Slide 1: Scintillator primary test results
Cunfeng Feng
Zhongquan Zhang
Ang Li

## Slide 2: Test results before the New Year holiday
scintillator number | no reflector |  |  | tyvek | mylar
 | air gap lead | print paper | print paper |  | 
 | no narrowside | no narrowside | narrowside |  | 
1 | 5.5 | 5.8 | 6.6 | 9.5 | 5.9**
2 | 4.4 | 4.7 | 6.25 | 8.3 | 5.3**
3 | 5.5 |  | 5.5* | 9.8 | 6.1
4 |  |  |  | 8.75 | 5.8
*:this scintillator has no reflector |  |  |  |  | 
**:these scintillators have no narrow side packages |  |  |  |  | 

## Slide 3: Test results after the New Year holiday
scintillator number | mylar | no reflector |  | 
 |  | no air gap lead | print paper | print paper*
 |  | no narrow side | no narrow side | no narrowside
1 | 5.3 | 4.4 | 4.8 | 6.1
2 | 4.5 | 3.1 | 4.5 | 5.2
3 | 5.6 |  | 5.5 | 5.5
4 | 5.6 | 5 | 5.2 | 
*:these results come from what we did before the New Year holiday |  |  |  | 

## Slide 4: Fit results
No.4
Mylar reflector
and narrow side
Before holiday
After holiday

## Slide 5
Thanks!