# EUROPEAN ORGANIZATION FOR NUCLEAR RESEARCH

11 December, 1998

TECHNICAL SPECIFICATION FOR WLS FIBRES PREPARATION, QC, DISTRIBUTION

Atlas Tilecal Collaboration

Item				: WLS (Wave Length Shifter) Fibres

PBS#				:  5.3.2.1

Quantity			:  about 960 Km

Date of delivery		:  May 1th, 1999 first batch aluminized

To be delivered to		:  LISBON

Institutes involved		:  LISBON, PISA

Document responsible		:  A. Maio

# Document due the 		:  November 30th, 1999

# 1- Introduction

The Tile Calorimeter is a sampling calorimeter with a cylindrical structure divided in modules, each module being a periodic structure. Submodules formed by layers of master steel plates alternating with layers of spacer steel plates and scintillating tiles compose each Module. The scintillating tiles are read out by WLS (Wave Length Shifter) optical fibres that at one top are connected with a PMT and at the other are aluminised to form a mirror that sends light back to the PMT increasing the efficiency of the Calorimeter.

To get a good mirror at the top of the fibres two steps must be followed, the first one is to obtained a flat surface with minimised roughness, the second step consists in coating the surface with a suitable metal that shall be high purity aluminium.

The flat surface is obtained by cutting with hot wire followed by milling device and polishing with a special diamond tool.

The Magnetron Sputtering technique has been chosen to produce the mirror at the top of the fibres because it produces thin films with good reflectivity, high adherence and good reproducibility in the results. Thermal evaporation in high vacuum could in principle give more 2 or 3% reflectivity. However it was excluded because it would produce a non-acceptable thermal stress to the fibres and would increase dramatically the vacuum requirements. The Magnetron Sputtering technique has also the advantage of depending on easily controllable parameters

The cold plasma parameters that influence the reflectivity of a thin film obtained by Magnetron Sputtering are the cleaning pressure, deposition pressure, discharge power and cathode-substrate distance. Film material and thickness, substrate temperature during deposition and substrate surface structure (roughness) can have also a big influence in reflectivity.

## 1.1- List of tasks

The list of all tasks, in the present configuration, is shown below:

- Bundling of the fibres and quality control

- Cutting of the bundles with hot wire and quality control

- Cutting of the bundles with a milling machine and quality control

- Polishing of the fibres with diamond tool and quality control

- Coating of the surface with Aluminium and quality control

Gloves are needed to handle the fibres in all tasks. Daylight and lights with high UV component must be avoided.

# 2- Bundling

To be cut and polished, the fibres must be grouped in bundles in order to get enough mechanical strength to support the transverse stress due the cut and polishing procedures.

The present baseline for the cut and polishing uses the fibres packed in hexagonal bundles. The hexagonal bundles are used because they also distribute in a better way the lateral forces to which the fibres are subjected inside the bundle. However bundling hexagonal rods (see drawing in appendix 1) is one of the most time expensive processes due to the fact that the rod needs to have exactly 1261 fibres in a hexagonal array. It takes about half a day to build one bundle of typical 2 m long fibres.

The optical fibres in this stage must have 1.5 cm more than the final length to take into account losses in hot wire cutting and in cases of bad polishing that oblige to repeat the process.

After all the fibres are in place they are tightened with a Dynamometer screwdriver with the strength of 18 N/m.

This task can be done by only 1 person, but to minimise the stress induced to the fibres should be performed by 2 persons. For this task it is required a 4 m long table.

The total number of bundles for 565 000 fibres will be about 448.

## 2.2- Quality Control for the hexagonal bundles

The Quality Control is made during the production of the bundles by visual inspection and by counting the number of fibres on each side of the hexagon, that has to be exactly 21.

## 2.3- Circular Bundles

In order to reduce the bundling time, the manufacture of circular bundles (drawing in appendix 1) is being explored.  Circular bundles can accommodate about 2900 fibres. Freezing the fibres together with water to a temperature enough to keep the water solid during cutting and polishing allows also to distribute the lateral forces and gives strength to the bundle. Moreover freezing contributes to give to the polymer a better viscoelastic behaviour of the fibres in these bundles. Preliminary results, not fully satisfactory, were obtained. New tests are in progress.

# 3- Cutting

The cutting process is made in two steps. In the first step, the fibres are cut with a hot wire that guarantees more mechanical resistance to the bundle for the second step, when the bundle is cut with a milling machine.

## 3.1- Cutting with Hot Wire

In order to avoid thermal damage to the fibres this process is made in several steps instead of cutting through the entire surface in only one step. After cutting with the hot wire the fibres are left 6 mm out of the top pieces of the bundle. This operation will be done in both sides of the bundle.

The specifications of the hot wire are the following:

Material of the wire					Metal Chromium/Nickel

Length							9 cm

Total length need for the full project			5 m

Diameter						0,5 mm

Electrical Current					3.8 A

Time spent for each face				5 minutes

## 3.2- Freezing the fibres in ice

In the case of using circular rods the top of the fibres are frozen in water using liquid nitrogen. When using this procedure the hot wire is not applied. Details will be given after the feasibility of the process is proven.

## 3.3- Cut with Milling Machine

The cut with the milling machine is done in several passages, cutting at most 1 mm in the first passages and 0.4 mm in the last ones. After the cut with the milling machine the fibres are left with 1 mm out of the top pieces of the bundle. This operation will be done in both sides of the bundle.

During this process small particles produced are removed using clean compressed air and aspiration.

A positioner to guarantee the perpendicularity between the rod and the milling machine is under study and will be implemented soon.

The best work conditions established at present are:

Tool rotation frequency		580 Rots/Minute

Bundle carriage advance speed	140 m/s

Material removal rate			0.4 mm/passage

Time spent for each face		40 minutes

One person is needed to perform this task, but help of one other is needed to carry the longest bundles between workstations (from bundling and cutting with hot wire to the milling machine and from this machine to store).

## 3.4- Quality Control

The Quality Control of the cutting process is done visually after the end of the milling procedure. The surface is observed to guarantee the regularity and smoothness of the fibre surface. Photography of the bundles can be implemented with quality control purpose.

# 4- Polishing

The fibres polishing is done by a tool composed by a steel and a diamond blade that alternatively attack the surface of the fibres. The steel blade is the first to attack the surface of the fibres followed by the diamond blade. This composed tool works in the same machine as the milling tool and uses the same equipment (aspiration and clean compressed air) and also the positioner already referred. The same positioner referred in 3.3 will be used in this operation. This operation will be done in both sides of the bundle.

Replacing the milling tool by the polishing tool and tuning it takes one day.

In the polishing process 0.1 mm of material is removed in each passage.

The best work conditions established at present are:

Tool rotation frequency		800 Rots/Minute

Bundle carriage advance speed	140 m/s

Material removal rate			0.1 mm/passage

Preparing the polish tool		1 day

Time spent for each face		40 minutes

One person is needed to perform this task, but the help of another is needed to carry the longest bundles between workstations (from store to the milling machine to polish and back to store).

## 4.1- Quality Control

The Quality Control of the polishing is done visually after the end of the process. The surface of the fibres is observed to guarantee its regularity and smoothness. Photography of the bundles can be implemented with quality control purpose.

# 5- Aluminization

The aluminization of the fibres is done by Magnetron Sputter Deposition in a high-vacuum system with high purity Aluminium (99.999%) on one of the top surfaces of the fibres.

The system is pumped by a turbomolecular, a diffusion and two rotary mechanical pumps delivering a pumping speed of 600 l/s at the fibre chamber and has the capacity to aluminize one bundle of about one meter in 8 hours.

The optimised working conditions for the aluminizations are:

Cleaning pressure		1.5x10-3 Pa

Pumping time			7 hours

Discharge pressure		5.0x10-1 Pa

Power				1 kW

Deposition rate		3.5 nm/s

Deposition time		75 s

Cathode/substrate distance	8 cm

Fibre temperature increase	2 ºC

Rate of production		1 bundle with 1m long fibres in 8 hours

In total 2 high purity targets will be used in the aluminization of 565 000 fibres. The targets have 5 mm of thickness and 65 mm of diameter.

## 5.1- Mass Production system

A mass production system to aluminize 4 bundles each cycle is being projected and constructed. This new system has two chambers, one for the aluminization, separated by a gate valve from the second chamber where the fibres will be degassed separately without poisoning the vacuum in the deposition chamber. The degassing chamber is pumped with 2 turbomolecular pumps with a combined pumping speed of 1000 l/s. The deposition chamber will be pumped with 380 l/s by a turbomolecular pump.

In each cycle 4 bundles, supported by a revolver system in the degassing chamber, will be degassed till the cleaning pressure and then successively admitted in the aluminization chamber to be coated. It is expected a production rate of 8 bundles a day. To achieve this production rate a drying/degassing system is being designed, consisting in a pumping system with a cool trap.

In average the rate of production with this system will be 8 bundles/day.

5.2 - Quality Control

The aluminization quality control consists in the measurement of the reflectivity of the polymer/aluminium interface. The optical quality control of about 5% of the fibres in each bundle will be performed by measuring the light yield at a fixed distance from the mirror, the attenuation length (quality control of fibres, PBS # 5.3.2.1.) and the reflectivity. The set up is the same used in the fibre quality control (chapter of fibres, PBS # 5.3.2.1.). These fibres will be taken from 2 perpendicular lines in the central region of the bundle. The removal of the fibres will be done in the aluminization station.

From our experience in Lisbon it is expected a reflectivity of about (755)% (section 5.2.1). These numbers will be reviewed after the quality control of the pre-series (4+3 bundles) that is being produced. A reflectivity of (7510)% is acceptable, resulting in variations of light output of the order of 6% for fibres with lengths in the range 1.5-2.1 m.

### 5.2.1- Summary of the present tests

The results obtained in past tests and in this pre-series are shown in table 1.

Table 1- Reflectivity obtained for several bundles of fibres aluminized in Lisbon.

|  | Mean Reflectivity (%) | rms | rms (%) | Nº of fibres tested |
| --- | --- | --- | --- | --- |
| Bundle 25 | 79 | 3.3 | 4.1 | 40 |
| Bundle 26 | 75 | 4.4 | 5.6 | 39 |
| Bundle 30 | 69 | 4.5 | 6.5 | 29 |
| Bundle 31 | 77 | 4.3 | 5.5 | 35 |
| Bundle 32 | 68 | 5.9 | 8.7 | 37 |
| Bundle 33 | 74 | 4.7 | 6.5 | 37 |
| Bundle 34 | 71 | 6.7 | 9.5 | 48 |
| Bundle 37 | 65 | 5.1 | 7.9 | 40 |

From the bundle 30 to the bundle 37 some spots of bad polishing has been observed in the surface of the bundles. Due to this fact the reflectivities in these bundles are below the best obtained. This problem is under study and will be solved soon. Due to the high number of fibres needed for these tests, all the bundles are made with old scintillating fibres plus a cross of WLS fibres, except bundle 37 that was made only with WLS fibres. The fibres used in bundle 37 where not perfectly cylindrical and their diameters showed fluctuations above the usual 1.000.02 mm.

The bundles 35 and 36 are being measured.

# 6- Bundle transport

The bundle transport will be done by placing the bundles inside PVC tubes with 70 mm of internal diameter. These tubes will be then placed in wooden boxes depending on the place they will be sent. About 800 m of the PVC tube will be needed for the production of 448 bundles.

# 7- Quality control summary

Table 2- Quality control summary

| Task | Visually | Photography | Reflectivity measurement |
| --- | --- | --- | --- |
| Bundling | X |  |  |
| Cutting | X | P |  |
| Polishing | X | P |  |
| Aluminization | X | P | X |

X- Already implemented

P- Will be implemented

# 8- Production rates

Bundling				2 bundles/day

Cutting with hot wire			6 bundles/hour

Cutting with milling machine		6 bundles/day

Replacing the tool			1 day

Polishing				6 bundles/day

Aluminization				8 bundles/day

The expected mass production schedule is shown below.

This schedule was done considering the following correspondences:

A day of work		8 hours 	A month		20 days

A year			10 months 	A week		5 days

# 9- Important figures

- General

- Total number of fibres to aluminised			565 000

- Bundling

- Total number of bundles					448

- The need of a table with length of			4 m

- Workers needed						2

- Extra length that fibres needed in this stage		1.5 cm

- Time spent for each bundle				0.5 day

- Cutting with hot wire

- Total length of wire needed for all production		5 m

- Time spent for each bundle (cutting both faces)		10 minutes

- Workers needed						1 (with help of other to place

the longest bundle in place)

- Milling machine cut

- Time spent for each bundle (cutting both faces)		80 minutes

- Machine active time					1 week each 7 weeks

- Workers needed						1 (with help of other to place

the longest bundle in place)

- Polishing

- Time spent for each bundle (cutting both faces)		80 minutes

- Machine active time					1 week each 7 weeks

- Workers needed						1 (with help of other to place

the longest bundle in place)

- Aluminization

- System active time					1 week each 7 weeks

- Time to aluminization					8 bundles/day

- Total number of high purity Aluminium			2

# 10- Contact persons

A. Maio

A. Wemans	Email: awmns@mail.telepac.pt

andre.do.valle.wemans@cern.ch

# 11- Notes

- All equipment described belongs to the project (LIP/LISBON)

- A Tilecal Technical note about these subjects is in preparation.

##### Appendix 1 – Drawings of the bundles

Hexagonal bundles

Circular bundles