## Slide 1: Scintillator test results
Cunfeng Feng
Zhongquan Zhang
Ang Li

## Slide 2: Structure of the experiment
Trigger
Group1
Group2
Group3
Group4
Reference
Trigger
PMT
PMT
PMT
PMT
PMT
PMT
PMT
DAQ
shelf

## Slide 3: Structure of each group
PMT
Aluminum plate
lead
scintillator
reflector
The reflectors are changed everyday, sometimes they are print paper, sometimes they are aluminum, sometimes they are Tyvek, sometimes they are nothing.

## Slide 4: Reflectors

## Slide 5: Data of reference
Reference
2016-04-17

## Slide 6: Results
Chart: Reference
| 42429 | 42430 | 42431 | 42432 | 42433 | 42434 | 42440 | 42446 | 42447 | 42448 | 42449 | 42450 | 42451 | 42452 | 42453 | 42454 | 42455 | 42456 | 42457 | 42458 | 42459 | 42460 | 42462 | 42463 | 42464 | 42465 | 42466 | 42467 | 42468 | 42469 | 42470 | 42471 | 42472 | 42473 | 42474 | 42475 | 42476 | 42477 | 42478 | 42479 | 42479
 | 31.6 | 31.3 | 30.7 | 30.1 | 28.9 | 28.9 | 27.6 | 25.7 | 25.4 | 25.1 | 26.1 | 25.7 | 26.3 | 25.1 | 26.7 | 25.5 | 27.1 | 28 | 26.8 | 27.1 | 27 | 27.4 | 29.1 | 29.5 | 29.6 | 30.3 | 28.3 | 29.8 | 30.8 | 31.7 | 31.3 | 30.1 | 30.7 | 31 | 32 | 30.3 | 30.2 | 30.1 | 30.7 | 30.3 | 29.9

## Slide 7: Results
Chart: without reflector
| 42429 | 42430 | 42431 | 42432 | 42433 | 42434 | 42440 | 42446 | 42447 | 42448 | 42449 | 42450 | 42451 | 42452 | 42453 | 42454 | 42455 | 42456 | 42457 | 42458 | 42459 | 42460 | 42462 | 42463 | 42464 | 42465 | 42466 | 42467 | 42468 | 42469 | 42470 | 42471 | 42472 | 42473 | 42474 | 42475 | 42476 | 42477 | 42478 | 42479 | 42480
Group1 | 25.7 | 24.9 | 26 | 24.5 | 24.9 | 26.7 | 24.2 | 24.4 | 24.6 | 30.6 | 29.6 | 25.7 | 24.2 | 23.1
Group2 | 27.4 | 25.8 | 26 | 22.9 | 21.3 | 24.1 | 23.7 | 23.4 | 22.4 | 26.1 | 27.4 | 24.3 | 24.5 | 22.1
Group3 | 28.6 | 27.4 | 27.1 | 26.3 | 26.6 | 25.8 | 25.3 | 24.6 | 29.5 | 25.2 | 21.4 | 20.4
Group4 | 28.4 | 26.7 | 27.1 | 24.7 | 24.1 | 23.8 | 22.9 | 22.9 | 21.9 | 30 | 29.2 | 24.2 | 27.2 | 21.7
Reference | 31.6 | 31.3 | 30.7 | 30.1 | 28.9 | 28.9 | 27.6 | 25.7 | 25.4 | 25.1 | 26.1 | 25.7 | 26.3 | 25.1 | 26.7 | 25.5 | 27.1 | 28 | 26.8 | 27.1 | 27 | 27.4 | 29.1 | 29.5 | 29.6 | 30.3 | 28.3 | 29.8 | 30.8 | 31.7 | 31.3 | 30.1 | 30.7 | 31 | 32 | 30.3 | 30.2 | 30.1 | 30.7 | 30.3 | 29.9

## Slide 8: Results
Chart: print paper
| 42429 | 42430 | 42431 | 42432 | 42433 | 42434 | 42440 | 42446 | 42447 | 42448 | 42449 | 42450 | 42451 | 42452 | 42453 | 42454 | 42455 | 42456 | 42457 | 42458 | 42459 | 42460 | 42462 | 42463 | 42464 | 42465 | 42466 | 42467 | 42468 | 42469 | 42470 | 42471 | 42472 | 42473 | 42474 | 42475 | 42476 | 42477 | 42478 | 42479 | 42479
Group1 | 28.9 | 29.8 | 30.9 | 29.5 | 25.5 | 28 | 25.9 | 22.8 | 25.1
Group2 | 33.9 | 31.6 | 28.9 | 28.7 | 27.6 | 27.6 | 24.1 | 26.3 | 25.5
Group3 | 34.7 | 32.9 | 33.5 | 32 | 27.5
Group4 | 32.1 | 32.4 | 32 | 27 | 29.9 | 26.4 | 24.8 | 29.8
Reference | 31.6 | 31.3 | 30.7 | 30.1 | 28.9 | 28.9 | 27.6 | 25.7 | 25.4 | 25.1 | 26.1 | 25.7 | 26.3 | 25.1 | 26.7 | 25.5 | 27.1 | 28 | 26.8 | 27.1 | 27 | 27.4 | 29.1 | 29.5 | 29.6 | 30.3 | 28.3 | 29.8 | 30.8 | 31.7 | 31.3 | 30.1 | 30.7 | 31 | 32 | 30.3 | 30.2 | 30.1 | 30.7 | 30.3 | 29.9

## Slide 9: Results
Chart: Aluminum
| 42429 | 42430 | 42431 | 42432 | 42433 | 42434 | 42440 | 42446 | 42447 | 42448 | 42449 | 42450 | 42451 | 42452 | 42453 | 42454 | 42455 | 42456 | 42457 | 42458 | 42459 | 42460 | 42462 | 42463 | 42464 | 42465 | 42466 | 42467 | 42468 | 42469 | 42470 | 42471 | 42472 | 42473 | 42474 | 42475 | 42476 | 42477 | 42478 | 42479 | 42479
Group1 | 28.8 | 27.8 | 27.7 | 27.2 | 25.9 | 24.3 | 29.2
Group2 | 28.7 | 27.7 | 27.5 | 28.9 | 27.5 | 23.2 | 27.2
Group3 | 34.7 | 35 | 34.8 | 31.4 | 31 | 28.1 | 30.4
Group4 | 31.6 | 30.6 | 29.5 | 29 | 30.1 | 29.2 | 30.7
Reference | 31.6 | 31.3 | 30.7 | 30.1 | 28.9 | 28.9 | 27.6 | 25.7 | 25.4 | 25.1 | 26.1 | 25.7 | 26.3 | 25.1 | 26.7 | 25.5 | 27.1 | 28 | 26.8 | 27.1 | 27 | 27.4 | 29.1 | 29.5 | 29.6 | 30.3 | 28.3 | 29.8 | 30.8 | 31.7 | 31.3 | 30.1 | 30.7 | 31 | 32 | 30.3 | 30.2 | 30.1 | 30.7 | 30.3 | 29.9

## Slide 10: Results
Chart: tyvek
| 42429 | 42430 | 42431 | 42432 | 42433 | 42434 | 42440 | 42446 | 42447 | 42448 | 42449 | 42450 | 42451 | 42452 | 42453 | 42454 | 42455 | 42456 | 42457 | 42458 | 42459 | 42460 | 42462 | 42463 | 42464 | 42465 | 42466 | 42467 | 42468 | 42469 | 42470 | 42471 | 42472 | 42473 | 42474 | 42475 | 42476 | 42477 | 42478 | 42479 | 42479
Group1 | 40.8 | 37.9 | 34.2 | 27.5 | 27 | 35 | 27.4 | 29.1
Group2 | 37.8 | 37.6 | 33.2 | 29.5 | 26.6 | 30.1 | 27.7 | 31.1
Group3 | 49.1 | 36.7 | 37.6 | 33.6 | 29.9 | 33.9 | 30.5 | 31.4
Group4 | 42.9 | 31.7 | 36.8 | 31.8 | 30.4 | 28.4 | 27.4 | 28.7
Reference | 31.6 | 31.3 | 30.7 | 30.1 | 28.9 | 28.9 | 27.6 | 25.7 | 25.4 | 25.1 | 26.1 | 25.7 | 26.3 | 25.1 | 26.7 | 25.5 | 27.1 | 28 | 26.8 | 27.1 | 27 | 27.4 | 29.1 | 29.5 | 29.6 | 30.3 | 28.3 | 29.8 | 30.8 | 31.7 | 31.3 | 30.1 | 30.7 | 31 | 32 | 30.3 | 30.2 | 30.1 | 30.7 | 30.3 | 29.9