## Slide 1: Test of reflective materials on lead surface
Botan Wang
Tsinghua University

## Slide 2: Test devices
PMT
C.A.E.N
N470
V
Beta source
+HV
Signal

## Slide 3: Lead sheet samples
New samples:
  Nanjing thin sheets (40-60mm)
  Nanjing thick sheets (40-80mm)
For comparison:
  Old smooth surface (36.5mm)
  New smooth surface (37.5mm)
  Thick TYVEK (62.5mm)

## Slide 4: Signal readout
Multimeter
  Read the voltage variation range
  Difficult to tell the difference
Digital Phosphor Oscilloscope (DPO4034B)
  High resolution mode: average output in a period of time, more smooth signals;
  1MΩ impedance to get the measurable voltage;
  Sampling frequency: 10 Samples/s, total number 10K for calculation

## Slide 5: Test result
 | Multimeter/mV | DPO/mV | Former Test/V
Old smooth surface | 41 (39~43) | 3.924 | 0.45 (0.44~0.49)
Nanjing thin Surface | 40 (38~42) | 4.127 | 
Nanjing thick Surface | 40 (37~43) | 3.749 | 
New smooth surface | 36 (33~39) | 3.463 | 0.45 (0.43~0.49)
Thick TYVEK | 47 (44~50) | 4.177 | 0.54 (0.52~0.56)
no resource | 3 (2~4) | 0.918 | 0.04 (0.03~0.05)